Butyl DIGlycol

Description

Butyl Di Glycol is a solvent in paint and surface coatings, as well as cleaning products and inks.

CAS NO. 112-34-5

MOL WT. 162.23

Specification

PHYSICAL STATE  : clear liquid

BOILING POINT : 230.6 C

FREEZING POINT : -70 C below

SPECIFIC GRAVITY : 0.952-0.956

SOLUBILITY IN WATER  : miscible

VAPOR DENSITY : 4.1

VAPOR PRESSURE : 0.01 mmHg, 20 C

VISCOSITY : 6.5 mPa s

AUTOIGNITION : 244 C

REFRACTIVE INDEX : 1.4316

FLASH POINT : 120 C

COLOR : 15 below APHA

WATER : max 0.1%

Packing

190kg drum