CD-80

Description

CD-80 is widely used as solvent and thinner. It has good solubility

Applications

Paint, Ink, Cleaning agent and wax solvent.

Specification

| Item | Specification | Unit | Test Method |
| --- | --- | --- | --- |
| Appearance | Clear |  | Visual |
| Specific Gravity, 15.56/15.56℃ | 0.818~0.822 |  | ASTM D4052 |
| Distillation -Initial Boiling Point -50% -End Point | Min. 205 Max. Max. 245 | ℃ | ASTM D86 |
| Flash Point | Min. 75 | ℃ | ASTM D93 |
| Anline Point | Max. 60 | ℃ | ASTM D611 |
| Sulfur Content | Max. 3 | wt-ppm | ASTM D5453 |
| Color Saybolt | +30 |  | ASTM D156 |
| Reaction Test | Around 1.4498 |  | ASTM D 1218 |
| Brome Index | 0 | mgBr2/100g | ASTM D 2710 |
| Water content | 16 ug/g |  | ASTM D 1744 |
| Copper Corrosion | Max. 1 |  | ASTM D130 |
| Kinematic Viscosity | Nm2/s, 40 ℃ | Min 1.5 | ASTM D 445 |
| Aromatic Content | Max. 0.5 | Wt % | UOP 495 |