# L-C 301E

## Physical Property

| Appearance | White Powder |
| --- | --- |
| Softening Point (Ring & Ball, ℃) | 100±3 |
| Melt Viscosity (Brookfield, cps @ 140℃) | 180±50 |
| Density (g/cm2) | 0.93 |
| Hardness (dmm) | Max 5 |
| Acid Value (mgKOH/g) | 16±2 |

## Applications

Processing aid for plastic(PVC), production of emulsion(textile, coating and floor polish), paint additives.

## Standard Packages

25Kg bag

## Safety Precaution

L-C Wax is regarded as non-hazardous when exposure is controlled by using accepted industrial hygiene practices. Consult our Material Safety Data Sheet for specific recommendations on safe handling.