###### PVC STABILIZER

< SINGLE STABILIZER>

| Name | Packing Unit | Features |
| --- | --- | --- |
| TLS (Tribasic Lead Sulphate) | 25KG/Sack 500KG/BAG | TLS is a representative product for kind of lead stabilizer for PVC. It is widely used for both flexible and rigid products, and mainly used for PVC compound for electric wires due to its outstanding function as an insulator. |
| DLP (Dibasic Lead Phosphite) | 25KG/Sack 500KG/BAG | DLP is good for exterior construction materials such as PVC window frame and PVC plate due to its weatherability, insulation and thermal stability and needs to be used in combination with Pb-St, DBL, and Ba-St. |
| DBL (Dibasic Lead Sterate) | 10KG/Sack | DBL shows a high quality in thermal stabilization, insulation, water resistance, blooming and bleeding and as a result, it can maintain activated state at high temperature. It is mainly used for PVC compound for electric wire and injecting and extruding products. |
| Pt-St (Lead Stearate) | 25KG/Sack | Holding excellent lubricity and thermal stability, Pb-St is mainly used for the soft extrusion and is suitable for both soft and rigid products, extrusion, injection and calender products. |
| Ba-St (Barium Sterate) | 20KG/Sack | Ba-St results a high activating effect and shows its excellence in thermal endurance, transparency and processibility. More synergy effect could be expected when it used in combination with Cd or Zn, soap, which could prevent an early pigmented change and extend the late thermal endurance. Ba-St is used for soft seat, leather, rigid pipe, and coating for electronic wires and cable. |
| Ca-St (Calcium Sterate) | 15KG/Sack 20KG/Sack | Ca-St shows its excellence in general gelation and gel luvricity. Because of its non-toxic features, it is used for non-toxic compounding with Zn-St. It is widely used as a lubricant and for food packing, film, sheet leather, rigid panel, pipe lubricant for rigid. extruding process. |
| Zn-St (Zinc Stearate) | 20KG/Sack | In spite of its excellence in non-toxicity and prevention of early pigmented change and plate-out, Zn-St has a weakness for zinc burring because of its low thermal stability. It is used for food packing, film, sheet, no-toxic product, and reginating anti-dditive for general olefin |
| DZ-10 (High Zinc Stearate) | 20KG/Sack | DZ-10 has the same application with that of Zn-St. In addition, it is mainly used for woodwork due to its excellence in transparency and dispersibility. |

<COMPLEX STABILIZER>

| Application | Composition | Appearance | Grade | Features |
| --- | --- | --- | --- | --- |
| Cable | Pb, Ba | Powder | KN-900 | - High resistance to heat - Excellent insulation |
| Rigid-pipe & Corrugated Pipe | Pb, Ca | Powder / Pellet | KN500 | - High work stability - High productivity - High permanent thermal stability |
| Window profile | Pb, Ca, Ba | Powder / Pellet | WP | - Good weatherability - Excellent permanent thermal stability |
| Tile | Pb, Ba, Zn | Powder / Pellet | DS-352 | - Good processibility - Good for early pigment |
| Fitting pipe | Pb, Ca, Ba | Powder | KN-506 | - Good processibility - Excellent productivity per unit time |
| Hose | Pb, Ca, Ba | Powder Pellet | NP | - Good thermal endurance - Good processibility |
| Nomal profile | Pb, Ca, Ba | Powder | KD-300 | - Good thermal enduring processibility |
| NON TOXIC | Zn, Ca, LDH | Powder | CZ | - Pb Free, Cd free, Good thermal endurance |

< LIQUID STABILIZAER >

| Product | Application |
| --- | --- |
| BC | BC class represents the Ba-Cd-Zn organic Complex and shows its superiority in thermal stability and transparency. It is used for both soft and hard calendar, film, seat and leather |
| BX | BZ class represents the Ba-Zn organic Complex, which is an one-pack-typed stabilizer wirh excellent lubricity. It is used for both soft and hard calendar, and foaming. |
| TIN | Tin class represents Dibutylitin Complex and shows its excellence in activity thermal endurance and weatherbility. It is used for both extruding and injection process stabilizer. |
| Stabilization additives | Stabilization preparations improve the transparency, thermal endurance and foam cell of processing products. |

< NON TOXIC STABILIZER BASED ON LDH (LAYED DOUBLE HYDROXIDE) >

| Application | Composition | Appearance |  | Features |
| --- | --- | --- | --- | --- |
| Cable compound | Ca, Zn, LDH | Powder | CZ-101 | . Good thermal stability . Good electric insulating property |
| Window profile | Ca, Zn, LDH | Powder | CZ-601 | . Good activation . Excellent thermal stability . Excellent light stability |
| Normal profile | Ca, Zn, LDH | Powder | CZ-301 | . Excellent weatherability . Excellent thermal stability |
| Rigid Pipe | Ca, Zn, LDH | Powder | CZ-500 | . Excellent weatherability . Excellent thermal stability, . Excellent processibility |
| Flexible Sheet | Ca, Zn, LDH | Powder | CZ800 | . Excellent weatherability . Excellent thermal stability, Excellent High Sheen |